## Slide 1: Study on fracture toughness and ductile-brittle transition based on interaction of cracks and dislocations
Tokyo University of Science
Keitaro Watanabe
Akiyuki Takahashi
Notes: I am
The title

## Slide 2
Background
Objectives
Analysis procedure
Numerical results
Consideration of fracture types
Conclusions
Notes: This slide is the table of contents for my presentation

## Slide 3: 2D dislocation simulation of BDT
Decoupled model
  Define macrocrack and microcrack in separate models
[1]
[1] S.J. Noronha, N.M. Ghoniem Metall. Mat. Trans. vol. 37 (2006) 539.
Calculation of microcrack fracture stress ()
① Microcrack simulation
② Macrocrack simulation
Calculation of fracture toughness ()
When
→
When
→

## Slide 4: Decouple model and coupled model
Feature of decoupled model
  The interaction between dislocations emitted from each crack is not considered
  The microcrack is subjected to only the uniform tension stress:
Advantage of coupled model
  Define macrocrack and microcrack in the same model
All interactions can be considered
① Macrocrack
② Microcrack
③ Emitted dislocations
Stress field of Macrocrack and dislocations of emitted from macrocrack

## Slide 5: Objectives
Investigate the detailed mechanism of fracture of microcracks near the macrocrack-tip using coupled model
Calculate the fracture toughness and ductile-brittle transition temperature

## Slide 6: Analysis procedure
② Emission of dislocations at crack-tip
④ Calculation of stress intensity factor
① Loading boundary condition on macrocrack
③ Calculation of force on dislocations
→ Dislocations emitted (Macrocrack blunting)
:Dislocation source
Calculate stress intensity factor from Peach-Koehler force at crack-tip
Calculation of macrocrack stress field
All interaction considered

## Slide 7: Coupled model
Analysis condition
Shear modulus[] | 
Poisson’s ratio [] | 
Burgers vector [] | 
Slip-plane angle [] | 
Surface energy [] | 
Critical value] | 
Applied load rate [] | 
Temperature [] | 
Crack length ] | 
Crack length [] | 
Ktip near
Ktip far

## Slide 8: Three fracture types of microcrack
(a)
(b)
(c) Crack closing

## Slide 9: Classification of fracture type
Brittle fracture process
[1]
[1] P.Bowen, S.G.D Druce, J.F.Knott Acta Mattall.
Vol. 34, No.6, pp.1121-1131, (1986)
Microcracks exist in material, mainly due to precipitates
Loading
① Blunting of macrocracks
② Microcracks cleave and
propagate to macrocrack
Brittle fracture requires microcracks propagate to macrocrack

## Slide 10: Three fracture types of microcrack
(a)
(b)
(c) Crack closing
Brittle fracture requires microcracks propagate to macrocrack
(a) has brittle feature
(b),(c) no propagation to macrocrack

## Slide 11: Fracture type mapping
Microcracks, which are the starting point of brittle fracture, are reduced
Increasing temperature decreases the area of brittle fracture

## Slide 12: BDTT
Fracture toughness vs. temperature
(a)
(b)
(a)
(b)
(a)
(b)
Fracture type shifts
at certain temperature
It is the limit temperature for fully brittle fracture
(b) Valid fracture toughness
value cannot be estimated
(a) Contribute to brittle fracture

## Slide 13: Why does fracture type shift?
Situations where the fracture type shifts
Crack length
Crack position
Temperature
Consider the main factors by checking four separate components ①Macrocrack, ②Macro dislocations, ③Micro dislocations near, ④Micro dislocations far

## Slide 14: Main factors that shift the type of fracture
Temperature
    Blunted macrocracks cause numerous dislocations to be emitted from microcrack-tip
    At high temperature, dislocations are emitted easily and macrocrack blunts more rapidly

## Slide 15: Temperature
At high temperature, microcrack is not subjected to strong tension from dislocations emitted from macrocrack

## Slide 16: Temperature
Effects from dislocations emitted from macrocrack
    Dislocations working in the shielding direction (
    (Black：positive Red：negative)

## Slide 17: Temperature
Effects from dislocations emitted from macrocrack
    Dislocations acting in the shielding direction (
    (Black：positive Red：negative)
Dislocations acting in the shielding direction increase

## Slide 18: Temperature
Effects from the macrocrack
Blunted macrocrack-tip increase
    Shear stress on microcrack (=Resolved shear stress for dislocation emission)
    Blunting of the macrocrack-tip causes numerous dislocations to be emitted from the microcrack-tip
    Blunting amount
High temperature
macrocrack blunted rapidly

## Slide 19: Temperature
at microcrack-tip
：Far dislocation emitted
：Near dislocation emitted
：
Same range
Same range
    At high temperature, dislocations are emitted easily

## Slide 20: Main factors that shift the type of fracture
Crack length
    Dislocations emitted from far side microcrack-tip shield the near side microcrack-tip
    Larger cracks have less this shielding effect

## Slide 21: Crack length
The macrocrack and dislocations emitted from macrocrack have little effect on the fracture

## Slide 22: Crack length
The effect of dislocations emitted microcrack-tip far side from macrocrack is strong

## Slide 23: Crack length
Effect of dislocations emitted from microcrack on crack-tip
The shielding effect decreases as the crack size increases

## Slide 24: Main factors that shift the type of fracture
Crack position
    Cracks near the macrocrack are subjected to strong tension and fracture before dislocations emitted from microcrack-tip
    Cracks near the macrocrack, the ratio of shielding effect to load is small

## Slide 25: Crack position
    Microcrack near the macrocrack are subjected to strong tension

## Slide 26: Crack position
Effects from the macrocrack
    Shear stress on microcrack
Blunted macrocrack-tip increase
The macrocrack fracture
before it can sufficiently blunt
under strong tensile loading
The macrocrack becomes
sufficiently blunted and releases numerous dislocations from the microcrack

## Slide 27: Conclusions
Coupled analysis was carried out for each crack length, position, and temperature
  Three different fracture types were obtained
Fracture toughness and transition temperatures were calculated
  Fracture toughness and transition temperature by assuming the conditions of a certain microcrack were obtained
Main factors that shift the type of fracture
  Temperature
    Blunted macrocracks cause numerous dislocations to be emitted from microcrack-tip
    At high temperature, dislocations are emitted easily and macrocrack blunted more rapidly

## Slide 28: Conclusions
  Crack length
    Dislocations emitted from far side microcrack-tip shield the near side microcrack-tip
    Larger cracks have less this shielding effect
  Crack position
    Cracks near the macrocrack are subjected to strong tension and fracture before dislocations emitted from microcrack-tip
    Cracks near the macrocrack, the ratio of shielding effect to load is small
Future perspective
  Extension of microcracks to 3D models assuming cracking of carbide particles (penny-shaped crack)

## Slide 29: Low-temperature embrittlement
Brittle-Ductile Transition:BDT
  Transition to ductile or brittle with temperature change
  Rapid decrease in fracture toughness at lower than the transition temperature
  Crack-dislocation interaction
[2]
[1]
[1] Tanaka, M., Sadamatsu, S., Journal of Materials Research,Vol 26, (2011)
[2] McMeeking, R.M. et.a, J. Mech. Phys. Solids 25, 1977
  Crack blunting
Main factors of BDT

## Slide 30: Crack-dislocation interaction
Shielding effect
    Stress intensity factor at crack-tip
    :Stress intensity factor due to external stress
    :Stress intensity factor due to emitted dislocations (-)
Shielding effect reduces stress concentration at crack tip BDT occurs at temperature where cleavage fracture does not occur
[1]
Total stress field
External stress
Emitted Dislocation
+
=
[1] Tanaka, M., Tarleton, E. and Roberts,S.G., Acta Materialia, Vol.56 (2008), pp.5123-5129.

## Slide 31: Crack-tip blunting
Blunting process
[1]
[1] X.H. Zeng. et al,Acta Materialia , 2009
Blunted cracks have high fracture toughness Microcracks fracture first and combine with macrocracks to progressively fracture
Crack-tip spread with curvature
Emitted dislocations become part of the crack-tip
Dislocations are emitted from the crack-tip

## Slide 32: Macrocrack model
Representation of crack-tip blunting
  Radius of curvature
Stress field near macrocrack tip
[1] McMeeking, R.M. et.al, J. Mech. Phys. Solids 25, 1977
[1]
: Number of dislocations
: Burgers vector
: Slip-plane angle
[6]
𝜌=𝑁𝑏𝑠𝑖𝑛𝛼

## Slide 33: Temperature dependence of dislocation
Dislocation emitted conditions
: Shear stress at dislocation source
Velocity of dislocations

## Slide 34: Microcrack model
Calculation of stress intensity factor
Creation of crack surface and calculation of stress intensity factor
Creation of crack surface
:Peach-Koehler force at crack-tip
: Shear modulus
: Poisson’s ratio
: Critical value
: Surface energy
: Crack length
: Stress of crack dislocations
Condition on crack surface：
：Move to a balanced position
：Fixed dislocation (crack-tip)
Determination of facture
Fracture begins

## Slide 35: Crack position
Effects from the macrocrack
Blunted macrocrack-tip increase

## Slide 36: Crack position

## Slide 37: Crack position
Shear stress in microcrack
  Dislocation source on the near side from the macrocrack
：Far dislocation emitted
：Near dislocation emitted
：

## Slide 38: Crack position
Shear stress in microcrack
  Dislocation source on the far side from the macrocrack
：Far dislocation emitted
：Near dislocation emitted
：

## Slide 39: Crack position
Stresses exerted by dislocation emitted from macrocrack on microcrack

## Slide 40: Temperature
Stresses exerted by dislocation emitted from macrocrack on microcrack

## Slide 41: Temperature
：Far dislocation emitted
：Near dislocation emitted
：
Shear stress in microcrack
  Dislocation source on the far side from the macrocrack

## Slide 42: Temperature

## Slide 43: Crack position
Effects from dislocations emitted from macrocrack
    Dislocations working in the shielding direction (
    (Black：positive Red：negative)

## Slide 44: Crack position
Effects from dislocations emitted from macrocrack
    Dislocations working in the shielding direction (
    (Black：positive Red：negative)
Dislocations acting in the shielding direction increase

## Slide 45: Crack position
σapp [MPa]
σapp [MPa]
    When microcrack is far away from macrocrack, the ratio of shielding effect to load is large